## Slide 1: Predicting bandgap in strain-engineered multinary III-V semiconductors
DPG-Frühjahrstagung (SKM) 2023
28/03/2023
Badal Mondal, Ralf Tonner-Zech
Wilhelm-Ostwald-Institute für Physikalische und Theoretische Chemie
Fakultät für Chemie und Mineralogie
Universität Leipzig

## Slide 2: Introduction
2
  Target optical property
    Bandgap (value, type)
    Bandgap tuning
Int. J. Sci (2014)
ACS Energy Lett. 5,611 (2020)

## Slide 3: Motivation
3
compositional engineering
strain engineering
compositional + strain engineering
  Comprehensive search experimentally not feasible
  Developing a predictive theoretical (computational) approach
    Composition-strain-bandgap map
Appl. Phys. A 69, 119 (1999)
Sci. Adv. 6, eabb0576 (2020)
Sci. Rep. 7, 46371 (2017)

## Slide 4: Approach
Computational details
  Density functional theory
    VASP
    Geometry optimization: PBE + D3(BJ)
    Electronic properties: TB09, SOC
    Binary systems (e.g. GaAs): primitive cell
    Ternary and quaternary systems (e.g. GaAsP): SQS (6 X 6 X 6)
  Machine learning
    Support vector machine-radial basis function kernel
isotropic strain
biaxial strain
uniaxial strain
P. Rosenow, L. C. Bannow, E. W. Fischer, W. Stolz, K. Volz, S. W. Koch, and R. Tonner,
Phys. Rev. B 97, 075201 (2018)

## Slide 5: Predicting bandgap in strain-engineered binary III-V semiconductors
Chapter 1

## Slide 6: Binary III-V systems
Strain-bandgap relationship: GaAs isotropic strain
∆EΓ = Eg
∆EΓ
Eg
B. Mondal and R. Tonner-Zech, arXiv:2208.10596 (2022)
direct-indirect
transition

## Slide 7: Predicting bandgap in strain-engineered ternary III-V semiconductors
Chapter 2

## Slide 8: Ternary III-V systems
Challenges
  Primitive cell
  Supercell
    Band folding
      Bandgap magnitude
      Bandgap nature?
Composition-strain-bandgap: Ga(As1-xPx)
Band unfolding
  Bloch spectral weight*
*S.-Y Yang et al., Adv. Phys:X 3, 1414631 (2018)
*V. Popescu, A. Zunger, Phys. Rev. b 85, 085201 (2012)
*

## Slide 9: Ternary III-V systems
Composition-strain-bandgap
Ga(AsP) isotropic strain
Bandgap phase diagram
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)

## Slide 10: Ternary III-V systems
Bandgap phase diagram
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
Ga(AsP) biaxial strain
Substrate effect

## Slide 11: Ternary III-V systems
Bandgap phase diagram: Ga(AsP) biaxial strain
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
direct bandgap

## Slide 12: Ternary III-V systems
Bandgap phase diagram: Ga(AsP) biaxial strain
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
direct bandgap
indirect bandgap

## Slide 13: Ternary III-V systems
Bandgap phase diagram: Ga(AsP) biaxial strain
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)

## Slide 14: Paradigm shift: DFT  DFT-ML
Accelerated mapping

## Slide 15: Paradigm shift: DFT  DFT-ML
Accelerated mapping
2,000
500,000
Strain=0
estimated required
# of DFT calculations

## Slide 16: Paradigm shift: DFT  DFT-ML
Accelerated mapping
Training
Training
Predictions

## Slide 17: Predicting bandgap in strain-engineered quaternary III-V semiconductors
Chapter 3

## Slide 18: Quaternary III-V systems
Machine learning model
  Supervised learning
    Support vector machine
    Radial basis function kernel
    Features: composition, strain
    Labels: bandgap (magnitude, nature)
Bandgap phase diagram
B. Mondal, J. Westermayr and R. Tonner-Zech, in preparation

## Slide 19: Quaternary III-V systems
Supervised machine learning
  SVM-RBF
  composition, strain, bandgap
Training (testing) set: 4000 points
Strain range: 5%
Prediction accuracy
  RMSE in bandgap values: 47 (1) meV
  Accuracy in bandgap nature: 95 (1) %
Ga(AsPSb) biaxial strain
Bandgap phase diagram
B. Mondal, J. Westermayr and R. Tonner-Zech, in preparation

## Slide 20: Quaternary III-V systems
Supervised machine learning
  SVM-RBF
  composition, strain, bandgap
Training (testing) set: 4000 points
Strain range: 5%
Prediction accuracy
  RMSE in bandgap values: 47 (1) meV
  Accuracy in bandgap nature: 95 (1) %
Ga(AsPSb) biaxial strain
Bandgap phase diagram
B. Mondal, J. Westermayr and R. Tonner-Zech, in preparation
direct-indirect transition
tensile
no direct-indirect transition
direct-indirect transition
compressive + tensile

## Slide 21: Quaternary III-V systems
Bandgap phase diagram: Ga(AsPSb) substrate effect
B. Mondal, J. Westermayr and R. Tonner-Zech, in preparation
Ga(AsPSb)/GaAs

## Slide 22: Summary
Strain-induced direct-indirect bandgap transition
Predictive composition-strain-bandgap mapping
  Bandgap phase diagram
Machine learning accelerated bandgap phase diagram
Binary
Ternary
Quaternary
Band unfolding
Machine learning
https://bmondal94.github.io/Bandgap-Phase-Diagram (find in contribution abstract)
direct-indirect
transition

## Slide 23: Acknowledgements
HRZ | Hochschulrechenzentrum
Prof. Dr. Ralf Tonner-Zech
Prof. Dr. Julia Westermayr
Prof. Dr. Kerstin Volz
Marcel Kröner
Thilo Hepp
https://bmondal94.github.io/Bandgap-Phase-Diagram (find in contribution abstract)

## Slide 24: Extra

## Slide 25: Ternary III-V systems
Bandgap phase diagram: Ga(AsP) biaxial strain
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
indirect bandgap
direct bandgap
X
X

## Slide 26: Bloch spectral weight
fold2Bloch: https://github.com/rubel175/fold2Bloch-VASP, last accessed 2022
Probability of finding a set of PC states contributing to SC state
Or,
The amount of Bloch character preserved in at the same energy
V. Popescu, A. Zunger, Phys. Rev. b 85, 085201 (2012)

## Slide 27: GaAs: isotropic compressive strain
(Γ : L : X) Bloch weights
Γ : L : X = 100:0:0
Γ : L : X = 50:50:0
Γ : L : X = 0:0:100
Direct bandgap
Direct-indirect transition
Indirect bandgap

## Slide 28: Direct-indirect transition
GaAs isotropic strain
GaAs0.963P0.037 isotropic strain

## Slide 29: GaAsP: Direct-indirect transition
(Γ : L : X) Bloch weights
GaAs0.963P0.037
isotropic compressive strain
GaAs0.63P0.37
Biaxial tensile strain
(Γ : [L or X]) Bloch weights

## Slide 30: GaAsP bandstructures
GaAs0.963P0.037: Isotropic compressive strain
Strain = 0.0%
Strain = −1.3%
Strain = −1.5%
Strain = −2.0%
Direct bandgap
Direct bandgap
Indirect bandgap
Direct-indirect
transition
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)

## Slide 31: GaAsN bandstructures
GaAs0.995N0.005: Isotropic strain
Strain = 0.0%
Strain = −4.5%
Strain = +4.5%
Strain = −5.0%
Indirect bandgap
Direct bandgap
GaAs0..889N0.111
Direct bandgap
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
Strain = 0.0%

## Slide 32: GaAsN bandstructures
GaAs0.995N0.005: Isotropic compressive strain band redefinition
Strain = −4.5%
Indirect bandgap
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
Γ : L : X Bloch weights

## Slide 33: Experimental comparison III-V binary systems
System | Unstrained bandgap (eV) |  | Isotropic strain DIT(%) |  | Transitions | 
 | Calculated | Experiment | Calculated | Experiment | Calculated | Experiment
Si | 1.19 | 1.17 | − | − | − | −
GaP | 2.36 | 2.34 | − | − | − | −
GaAs | 1.47 | 1.52 | −1.56 | −2.75 | Γ→L | Γ→X
GaSb | 0.64 | 0.81 | −1.00 | −1.54 | Γ→L | Γ→L
InP | 1.43 | 1.42 | −4.40 | −5.16 | Γ→X | Γ→X
InAs | 0.36 | 0.39 | −7.41 | −8.25 | Γ→X | Γ→X
InSb | 0.03 | 0.24 | −5.18 | −4.23 | Γ→L | Γ→X
B. Mondal and R. Tonner-Zech, arXiv:2208.10596 (2022)
*RMSE = 0.11 eV
*RMSE = 0.03 eV
*RMSE = 0.88%

## Slide 34: Experimental comparison III-V ternary systems
System | Substrate | Layer thickness (nm) | Bandgap RMSE (eV)
GaAsP | GaAs | ~10000 | 0.01
GaPSb | GaAs, GaP, GaSb | − | 0.10
GaAsSb | GaAs | ~50 | 0.13
GaAsBi | GaAs | ~50 | 0.10
GaAsN | GaAs | ~10 | 0.12
GaPSb | Si | ~8 | Indirect bandgap
GaPBi | GaP | ~50 | Indirect bandgap
GaAsSb | GaAs | ~4 | 0.42
GaAsN | GaAs, Si | ~6 | 0.66
B. Mondal, M. Kröner, T. Hepp, K. Volz and R. Tonner-Zech, arXiv:2302.14547 (2023)
QW heterostructures
RT-PL
XRD

## Slide 35: ML predictions analysis: Ga(AsPSb) biaxial strain
B. Mondal, J. Westermayr and R. Tonner-Zech, in preparation
Test set
All input data
Test set
All input data